## Slide 1: Decarbonizing Steel
Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner
13 March 2024

## Slide 2: Steel sector overview: The problem

## Slide 3: Key messages Steel sector overview
The global steel sector is responsible for approximately 10% of global CO2e emissions
  Global steel emissions have more than doubled since 2000 (from 1.2 gigatonnes in 2000 to 2.5 gigatonnes in 2021). However, emissions have started to decouple from production levels since 2016
  Without intervention, emissions are expected to continue growing due to rising demand from emerging economies. Reaching net zero by 2050 would require a 25% emission reduction by 2030
Steel is currently produced through three main production routes, all of which emit CO2:
  Blast furnace-basic oxygen furnace (BF-BOF): 72% of global steel production. It uses coke and limestone to produce pure iron from iron ore in a blast furnace, which is then turned into steel in an oxygen furnace
  Scrap electric arc furnace (scrap EAF): 21% of global steel production. Scrap metal is melted in an EAF using electrical energy
  Natural gas-based direct reduced iron-electric arc furnace (NG DRI-EAF): 7% of global steel production. Iron ore is turned into iron using natural gas, which is then melted in an EAF to produce steel
On average, BF-BOF is the cheapest production method ($390 per tonne vs. $415 for scrap EAF and $455 for NG DRI-EAF). However, regional variations in costs (such as for raw material and fuel) make all three methods competitive
Because steel is a 100% recyclable material, increased use of scrap metal can help decarbonize the steel sector
Downstream activities after crude steelmaking (e.g., refining, casting, rolling) represent less than 20% of the total steel production emissions
Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu

## Slide 4: Steel sector scope 1 and 2 emissions are ~10% of global emissions
40%
20%
80%
0%
100%
60%
Agricultural fuel combustion 4%
Crops
28%
Oil 4%
Land use, land-use change, and
forestry 14%
CO2e emissions in 2021: 50.1 billion tonnes
Livestock
33%
Natural gas
22%
Waste
21%
Agriculture, land use, and waste
Power and heat
Aviation 9%
Cement
17%
Marine 11%
Coal
74%
Other 2%
Chemicals
13%
Rail 1%
Industry
Road
77%
Transport
Oil and gas
20%
Commercial
combustion
21%
Commercial combustion 7%
HFCs from
refrigeration
and A/C
25%
Refining 4%
Residential
combustion
54%
Buildings
29%
29%
20%
15%
7%
Iron and steel
16%
Remaining industries
19%
Non-ferrous metals 2%
Non-metallic minerals 2%
Iron and steel
17%
Scope 1
Scope 2
Sources: Scope 1 emissions from Rhodium Group ClimateDeck (September 2023); Scope 2 iron and steel estimate from IEA (2023). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu

## Slide 5: Global steel emissions have more than doubled since 2000, with emission growth decoupled from production growth after 2016
Chart: 
 | 1.2377 | 1.2212 | 1.2401 | 1.305 | 1.3847 | 1.4997 | 1.5971 | 1.7643 | 1.7947 | 1.8037 | 2.0083 | 2.1675 | 2.1998 | 2.2949 | 2.3854 | 2.3237 | 2.2607 | 2.2838 | 2.4105 | 2.4624 | 2.3883 | 2.5173
 | 850 | 852 | 905 | 971 | 1063 | 1148 | 1250 | 1350 | 1345 | 1241 | 1435 | 1540 | 1563 | 1653 | 1675 | 1624 | 1633 | 1737 | 1828 | 1877 | 1882 | 1962
1
2
3
4
0
0
500
1,000
1,500
2,000
Global steel production (in million tonnes)
’00
‘01
’02
‘03
‘04
Global CO2e emissions from iron and steel production (in gigatonnes)
‘06
’07
‘08
‘09
‘10
‘11
‘12
‘13
‘14
‘15
‘16
‘17
‘18
‘19
‘20
‘21
‘05
Steel production
Iron and steel production emissions
Global CO2e emissions decoupled from steel production post-2016
Note: The majority of the world’s iron is used to make steel. Sources: Rhodium Group ClimateDeck (September 2023); World Steel Association; McKinsey, Decarbonization Challenge for Steel; IEA, CO2 Emissions in 2022, Reuters, China 2021 Crude Steel Output. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Observations
In recent years, the steel industry has made efforts to reduce its carbon footprint with more energy-efficient processes and technologies
  Though not enough by itself, recycling rates have improved (sitting around 80%-90% globally)
  Better manufacturing yields have made supply chains more efficient
  Enhanced control processes and predictive maintenance strategies have led improvements in operational efficiency
China, the largest steel producer in the world, saw a 3% decline in steel output in 2021 and a similar decline in the years since

## Slide 6: Crude steel is now produced through three main methods that all emit CO2:
Blast furnace-basic oxygen furnace (BF-BOF), which alone produces ~80% of iron & steel CO2
Scrap electric arc furnace (EAF), limited to recycled scrap
Natural gas-based direct reduced iron-electric arc furnace (NG DRI-EAF) most expensive, least used
1
2
3

## Slide 7: Of three main steelmaking methods, blast furnace-basic oxygen furnace (BF-BOF) is the cheapest, most popular, and most polluting
Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
BF-BOF ~73% of global steel production and ~80% of iron and steel CO2 emissions
Iron ore
Iron
Steel
2.33 tonnes of CO2 per tonne of steel
FeO2 + coal = Fe + CO2
1
Observations
BF-BOF: Iron ore, coke, and limestone produce iron in a blast furnace, which is turned into steel in an oxygen furnace

## Slide 8: Of the three main steelmaking methods, scrap electric arc furnace (EAF) is the cleanest, though limited by the scarcity of scrap material
More than 80% of steel recycled; scrap EAF accounts for ~22% of global steel production
Iron ore
Iron
Steel
Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Produces 0.66 tonnes of CO2 per tonne of crude steel, 72% less than BF-BOF
Takes collected scrap steel as input into an EAF
2
Observations
BF-BOF: Iron ore, coke, and limestone produce iron in a blast furnace, which is turned into steel in an oxygen furnace
Scrap EAF: Scrap metal is melted in an EAF using electrical energy

## Slide 9: Of the three main steelmaking methods, natural gas-based direct reduced iron-electric arc furnace (NG DRI-EAF) is the most expensive and least used
Iron ore
Iron
Steel
BF-BOF ~73% of global steel production and 80% of iron and steel CO2 emissions
Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Produces 1.39 tonnes of CO2 per tonne of crude steel, 40% less than BF-BOF
Uses natural gas, a cleaner reduction agent than coal
3
Observations
BF-BOF: Iron ore, coke, and limestone produce iron in a blast furnace, which is turned into steel in an oxygen furnace
Scrap EAF: Scrap metal is melted in an EAF using electrical energy
NG DRI-EAF: Iron ore turns into iron using natural gas, which is then melted in an EAF to produce steel

## Slide 10: At present, crude steel is produced through three main methods that all emit CO2: BF-BOF, scrap EAF, and NG DRI-EAF
Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
 | Blast Furnace-Basic Oxygen Furnace (BF-BOF) | Scrap Electric Arc Furnace (Scrap EAF) | Natural Gas-Based Direct Reduced Iron – Electric Arc Furnace (NG DRI-EAF)
Description | Iron ore, coke, and limestone produce pure iron in a blast furnace, which is turned into steel in an oxygen furnace | Scrap metal is melted in an EAF using electrical energy | Iron ore is turned into iron using natural gas, which is then melted in an EAF to produce steel
Main inputs | Iron ore, cooking coal | Scrap steel, electricity | Iron ore, natural gas
% of global steel production | 72% | 21% | 7%
CO2 per tonne of crude steel | 2.3 tonnes | 0.7 tonnes | 1.4 tonnes
Energy intensity per ton of crude steel | ~24 GJ | ~10 GJ | ~22 GJ
Average cost per tonne of crude steel | ~$390 | ~$415 | ~$455
Chart: 
 | 5 | 95
Chart: 
 | 22 | 78
Chart: 
 | 73 | 27
3
2
1

## Slide 11: BF-BOF is the cheapest, most popular, and most polluting process which relies heavily on coal
Blast Furnace-Basic Oxygen Furnace (BF-BOF)
Source: MIDREX (2021), ArcelorMittal (2021), World Steel Association (2021), IEEFA (2022), IEA Iron and Steel Technology Roadmap (2020). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Source: AcelorMittal
Process description
In the first step, coking coal and limestone is mixed with iron ore in a Blast Furnace (BF) to perform iron reduction and obtain molten crude iron
Crude iron is sent to Basic Oxygen Furnace (BOF) to be converted into cast iron
  At this stage, up to 30% scrap steel can be added
Observations
BF-BOF accounts for 72% of global steel production
  China, the world’s #1 steel producer, accounts for >50% world output and uses BF-BOF for 90% of steel production
Both steps in the BF-BOF process produce CO2 as a byproduct. On average, BF-BOF emits 2.3 tonnes of CO2 per ton of crude steel – the highest amount of the three conventional steel routes
BF-BOF remains cheapest means of steelmaking, with average production cost of $390/tonne

## Slide 12: Scrap EAF is a cleaner steel making method that uses an Electric Arc Furnace to recycle scrap steel
Blast Furnace-Basic Oxygen Furnace (BF-BOF)
Source: MIDREX (2021), ArcelorMittal (2021), World Steel Association (2021), IEEFA (2022), IEA Iron and Steel Technology Roadmap (2020), Columbia Center on Global Energy Policy (2021). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Source: AcelorMittal
Process description
Scrap EAF takes collected scrap steel as input
An Electric Arc Furnace (EAF) converts electricity into heat which is used to melt scrap steel into crude steel
Observations
Scrap EAF accounts for 21% of global steel production, but use of technology is limited by the scarcity of scrap material
Cleanest conventional route, emitting 0.7 tonnes of CO2 per ton of steel (72% less than BF-BOF)
  EU and US lead in scrap EAF production, accounting for ~40% of their steel production
Scrap EAF average cost of production of $415/ton – but cost fluctuates based on scrap and electricity prices

## Slide 13: DRI-EAF is less common and uses natural gas to reduce iron ore to pure iron, which then enters into an EAF to make crude steel
Natural Gas-Based Direct Reduced Iron – Electric Arc Furnace (NG DRI-EAF)
Source: MIDREX (2021), ArcelorMittal (2021), World Steel Association (2021), IEEFA (2022), IEA Iron and Steel Technology Roadmap (2020). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Source: AcelorMittal
Process description
Iron ore is mixed with natural gas in a Direct Reduced Iron (DRI) shaft to perform iron reduction and obtain pure iron
The iron is then fed into an Electric Arc Furnace (EAF) where it is converted into crude steel
Observations
DRI-EAF accounts for remaining 7% of global steel production and is most dominant in the Middle East and Africa, where gas is cheap and abundant
Natural gas is a cleaner reduction agent than coal. DRI-EAF on average emits 1.4 tons of CO2 per tonne of crude steel, 40% less than BF-BOF
DRI-EAF is the most expensive conventional production route at $455/ton

## Slide 14: India is one of the fastest growing steel producers, and set to continue use of blast furnaces to meet rapid demand
India’s new crude steel production capacity (2021 – 2038E)
Source: India Steel – The Indian Steel Industry. Climate Policy Initiative – Taking Stock of Steel. Credit: Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Chart: 
 | 8.1056 | 2.4146 | 32.2374 | 11.0667 | 8.2933 | 23.8244 | 23.9159 | 57.2785 | 3.1773 | 2.3354 | 2.8731 | 5.6184
 | 6.2088 | 0 | 1.012 | 0 | 0 | 0 | 4.1393 | 0 | 0 | 0 | 1.3798
 | 0 | 5.0595 | 0 | 0 | 0 | 0 | 0.13818 | 0 | 0 | 0 | 9.6582
 | 0 | 2.4146 | 20.3291 | 1.012 | 1.6557 | 0 | 0 | 33.1146 | 0 | 0 | 0
New crude steel production capacity in India ’announced’ or ‘under construction’ (in million tonnes per annum)
2021
2022
2023
1
2024
1
2025
2
2026
2028
2029
2030
2032
2036
1
2038
8
9
40
32
9
25
24
62
36
2
3
17
Integrated BF + BOF
Integrated DRI (coal) + EAF
Integrated BF/DRI (coal) + BOF/EAF/IF
Other
Observations
India is now the world’s second largest producer of crude steel, and it has typically been a net exporter post FY2016-17, apart from economic downturns
Because of continued investment, India’s steel making capacity is expected to hit 300 mm tonnes per annum by 2030-31
  To meet demand, India is set to build at least 200 MTPA of new fossil-fuel based, emission-intensive steel production capacity over the next 15 years
  68% of this capacity is expected to be blast furnaces
  Remaining 32% expected to be from other processes like integrated BF + BOF

## Slide 15: Global iron and steel emissions expected to rise without intervention; future reduction scenarios will require drastic cuts
Chart: 
 | 2.66 | 2.7
 | 2.3883 | 2.3 | 1.2
 | 1.78 | 0.22
0.0
0.5
1.0
1.5
2.0
2.5
3.0
3.5
Direct CO2 emissions in the iron and steel sector per IEA scenario (in Gt Co2 per year)
2020
2030
2050
2.4
Baseline
90% reduction by 2070 (IEA)
Net Zero Emissions by 2050 (IEA)
Only with intervention will CO2e from iron and steel decline into 2050
Notes: Baseline scenario reflects the policies and implementing measures that have been adopted as of September 2022 NZE = Net Zero Emissions. Source: IEA (2020), IEA Net Zero by 2050 (2021), IEA Iron and Steel Technology Roadmap (2020), McKinsey (2023). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Observations
If no action is taken, global emissions from the iron and steel sector are expected to peak at 2.7 gigatonnes per year in 2050
  Increase in emissions attributable to growing steel demand from emerging economies
  Over time, gradual shift in demand is expected from China to India, Southeast Asia and Africa
The International Energy Agency (IEA) has developed several possible pathways for the steel industry:
  In the 90% reduction by 2070 pathway, emissions would still need to drop by 50% by 2050
  In the net-zero emissions by 2050 pathway, emissions would already need to drop by 25% by 2030, and drop to close to zero by 2050

## Slide 16: BF-BOF is the cheapest production method, but regional cost differences impact margins across production methods
28%
Chart: 
 | 180 | 330 | 300 | 340 | 200 | 405
 | 90 | 130 | 30 | 170 | 90 | 185
 | 55 | 40 | 75
 | 65 | 45 | 90
100
200
300
400
500
600
700
0
Simplified levelized cost breakdown of crude steel production via conventional routes (in USD per tonne, 2020)
46%
23%
14%
17%
BF-BOF
72%
7%
10%
Scrap EAF
44%
20%
16%
20%
DRI-EAF
Avg. 2019
steel price*
390
460
415
510
455
590
11%
Raw materials
Fuel
Fixed OPEX
CAPEX
Regional cost variations
(*) Average steel price based on Hot Rolled Coil Steel Futures Continuous Contract (HRN00), average of 2019 monthly prices. Source: MarketWatch (2019) McKinsey,IEA Iron and Steel Technology Roadmap (2020), European Commission Joint Research Centre Science for Policy Report (2016). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Regional cost differences cause all steel making methods to be competitive
  Raw material and fuel costs typically make up 60-80% of production costs
Observations
Profit margins across the industry are slim – the average EBITDA margin of steel producers over the past 10 years was 8-10%
Raw material and fuel prices can cause strong fluctuations in margins, given that these typically make up between 60-80% of total production costs
  While some of these markets are global (iron ore), others are more regional (e.g. electricity, scrap steel) which can drive regional cost differences
Labor costs, feeding into fixed OPEX, are typically higher in advanced economies than in emerging economies
CAPEX for production equipment is usually consistent across regions. However, engineering, procurement and construction costs can vary significantly

## Slide 17: Downstream activities post-crude steelmaking use process heat and represent <20% of total steel production emissions
Molten, Base Crude Steel
Metallurgy & Refining Stage
Refined Steel Grades
Semi-Finished Products: Slabs, Billets, Blooms
Carbon (“Structural”) Steel
Alloy Steel
Stainless Steel
Tool Steel
Continuous Casting
Low to high carbon steels
Strong, durable, & affordable
Uses: building & construction, manufacturing
Low to high alloy steels
Easily machinable, heat & corrosion resistant
Uses: oil & gas pipelines, auto panels, kitchenware
10%-20% of chromium, nickel, or molybdenum
Corrosion resistant, low maintenance, sanitary
Uses: medical devices, food processing
Designed specifically for tools & dies
Hard & wear-resistant
Uses: cutting & drilling equipment, auto cylinder heads, aerospace blades
Hot-Rolled Products: Coils, Plates, Sections, Tubes, Rods, Wires, etc.
Final Rolling
Downstream steelmaking process
Source: World Steel Association, Association for Iron & Steel Technology, Eziil, Industrial Metal Supply, Steel Manufacturer’s Association Steelmaking Emissions Report (2022). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Observations
On average, <20% of steelmaking CO2 emissions come from downstream processes
Metallurgy involves adding alloys in hot ladle to convert base crude steel into different types of refined steel (carbon, alloy, stainless, or tool)
  Common alloys: manganese, chromium, cobalt, nickel, tungsten, molybdenum, vanadium
  Refining step traps and removes impurities through processes like stirring molten steel with gas like argon
  Continuous casting molds liquid steel into semi-finished products, usually slabs, billets, or blooms
  Finally, the steel goes through a number of different finishing processes (e.g. hot or cold rolling, galvanizing) depending on the intended end use of the steel

## Slide 18: Steel 100% recyclable material; increased use of scrap in primary and secondary routes expected to help decarbonize sector
Source: World Steel Association (2020), World Steel Association Scrap use in the steel industry (2021), World Steel Association Fact sheet: Raw materials in the steel industry (2023), Net Zero Steel (2021), Mission Possible Partnership Net Zero Steel Sector Transition Strategy (2021), IEEFA (2021), World Economic Forum (2023). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Source: World Steel Association
Observations
Steel is 100% recyclable and can be infinitely reused. Its magnetic properties allow easy separation from waste streams
Scrap EAF lowest-CO2 is the least emitting and least energy intensive conventional route and is also cost competitive
  As a share of steelmaking, Scrap EAF expected to grow from 22% today to almost 50% by 2050 in Net Zero scenario
  Use of scrap as additional metallic inputs in conventional BF-BOF and DRI-EAF possible and proven: EAFs can use up to 100% of steel scrap, and BOFs up to 30%
  Scrap separated into two categories: pre-consumer scrap (scrap from downstream steel manufacturing) and post-consumer scrap (~50/50 split)
  As a share of steelmaking, Scrap EAF expected to grow from 22% today to almost 50% by 2050 in Net Zero scenario
  Over 85% of steel is recycled today, world’s most recycled material. Scrap steel supply only grows as steel products become obsolete
  The scrap steel market is already well-functioning, and expectations are that as scrap becomes more expensive there will be more incentives to recover steel from difficult applications such as foundations

## Slide 19: Among major steel producing countries and regions, Asian economies lag in scrap steel consumption
Chart: 
 | 86.26 | 69.24 | 57.58 | 41.8 | 40.18 | 36.05 | 35 | 35 | 32 | 22 | 21.9
0
20
40
60
80
100
Scrap steel consumption as a share of crude steel production by major producing countries and regions (in %)
Turkey
USA
EU-27
Russia
South Korea
Japan
Africa
Central & South America
Middle East
India
China
Global average
58
36
35
35
Crude steel share of global production
2% | 4% | 7% | 4% | 3% | 5% | 1% | 3% | 3% | 7% | 54%
Scrap steel consumption varies regionally but lags places like India and China
Source: Bureau of International Recycling World Steel Recycling in Figures 2017-2021 (2021), IEA Iron and Steel Technology Roadmap (2020), World Steel Association Scrap use in the steel industry (2021), World Steel Association World Steel in Figures 2023 (2023), IEEFA New From Old: The Global Potential for More Scrap Steel Recycling (2021). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Observations
Average lifespan of a steel product is ~40 years, but with a wide range. Steel packaging (such as tin-coated steel cans) lasts only a few weeks on average, while steel used for buildings may last 100 or more years
This long life-span means that scrap steel is still scarce in emerging economies, as these countries industrialized later
Usually, local scrap steel recycling markets feed the domestic steel industry. But there is some international trade taking place:
  Turkey, the world’s 7th largest steel producer, imported over 90% of their scrap steel inputs
  The EU and the US are both large exporters of scrap steel

## Slide 20: Scrap steel stock is expected to continue growing globally, allowing for more markets to increase scrap steel recycling
(*) Canada, Mexico and USA. Source: World Steel Association (2018), World Steel Association Scrap use in the steel industry (2021), IEEFA New From Old: The Global Potential for More Scrap Steel Recycling (2021). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Chart: 
 | 320 | 350 | 380
 | 200 | 300 | 500
 | 230 | 370 | 460
Global scrap steel availability by major regions, 2017-2050 (in mm)
2017
2030
2050
750
1,020
1,340
EU + NAFTA* + Japan
China
Rest of world
Growing amount of scrap steel to alleviate demand in emerging economies like China
Observations
Domestic scrap availability to increase significantly in emerging economies over the coming years
  As China matures, it is expected to fuel much of global scrap steel supply through 2050
Today, steel stock in OECD nations has reached 12-13 tonnes per capita, while in India and Africa this is only 1 tonne per capita – meaning less scrap steel is likely to become available in India and Africa over time
As scrap availability improves, adoption of Scrap EAF and a growing share of scrap steal in total steel production become more feasible

## Slide 21: Steel Decarbonization Technologies

## Slide 22: Key messages Steel decarbonization technologies
Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Several emerging deep decarbonization steelmaking technologies now exist:
  Green hydrogen DRI-EAF: hydrogen produced using zero-carbon electricity is used as iron ore reductant instead of natural gas. Second step still uses an Electric Arc Furnace (EAF)
  Iron ore electrolysis: use of electricity to split pure iron from iron ore. Two technologies:
    Molten Oxide Electrolysis (MOE): a high current is run through a mixture of iron ore and a liquid electrolyte. The current causes the iron ore to split into oxygen and molten iron
    Electrowinning-EAF (EF-EAF): iron from iron ore is dissolved in an acid, which leaves behind impurities. The iron-rich solution is electrocuted to form pure solid iron, which is melted in an EAF
  Carbon Capture, Utilization and Storage (CCUS): BF-BOF and DRI-EAF can be retrofitted with point capture equipment. Captured carbon is then used or stored
These technologies produce steel with over 90% less CO2 emissions compared to conventional processes. However, green hydrogen DRI-EAF and CCUS BF-BOF / DRI-EAF come at a green price premium. CCUS is also less viable for BF route given difficulty to capture all carbon that’s released. Electrolysis may be cheaper than conventional processes, but has not been tested at scale yet
There are also some emerging transitional steelmaking technologies with lower decarbonization potential:
  Modifications to existing BF-BOF and DRI-EAF: using biomass as input, switching to zero-carbon electricity, partial green hydrogen injections
  Different production process: Smelting Reduction-BOF (SM-BOF)
Decarbonization potential of transitional technologies ranges between 10-50%, while they still come with a considerable green premium

## Slide 23: Most steel production uses BF-BOF, scrap EAF, and NG DRI-EAF, with Green H2 DRI-EAF, iron ore electrolysis, and CCUS technologies emerging
Iron ore
Iron
Steel
BF-BOF: Iron ore, coke, and limestone produce iron in a blast furnace, which is turned into steel in an oxygen furnace
Scrap EAF: Scrap metal is melted in an electric arc furnace using electrical energy
NG DRI-EAF: Iron ore turns into iron using natural gas, which is then melted in an EAF to produce steel
Green H2 DRI-EAF: Green hydrogen replaces natural gas as an iron ore reductant; water instead of CO2 is generated as a byproduct
Iron ore electrolysis: Molten oxide electrolysis runs a current through iron ore and liquid electrolyte to split ore into pure molten iron; electrowinning-EAF dissolves iron from iron ore in acid, then electrifies it from solid iron
Carbon capture, utilization, and storage (CCUS): Equipment is added to existing steel-producing infrastructure to capture emitted CO2, which is then sequestered or reused
See glossary. Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
2
1
3

## Slide 24: Green H2 DRI-EAF is an emerging technology using green hydrogen instead of natural gas as an iron ore reductant with standard electric arc furnaces
Green H2 direct reduced iron-EAF has an average cited decarbonization potential of ~90%
Iron ore
Iron
Steel
Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Renewable electricity is used throughout the production process, including the creation of green hydrogen
Comes at a green price premium
1
Observations
BF-BOF: Iron ore, coke, and limestone produce iron in a blast furnace, which is turned into steel in an oxygen furnace
Scrap EAF: Scrap metal is melted in an EAF using electrical energy
NG DRI-EAF: Iron ore turns into iron using natural gas, which is then melted in an EAF to produce steel
Green H2 DRI-EAF: Green hydrogen replaces natural gas as an iron ore reductant; byproduct is water vs. CO2

## Slide 25: Iron ore electrolysis is an emerging technology that uses an electric current to drive a chemical reaction, producing molten iron or pure solid iron
Iron ore electrolysis has an average cited decarbonization potential of ~97%
Iron ore
Iron
Steel
Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (13 March 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Iron is now akin to solid-state battery, allowing for a reversed process that produces electricity
Electrowinning-EAF dissolves iron from iron ore in acid, then electrifies it to form pure solid iron; molten oxide electrolysis runs a current through iron ore and liquid electrolyte to split ore into pure molten iron
May be cheaper than conventional processes but has not yet been proven at scale
2
Observations
BF-BOF: Iron ore, coke, and limestone produce iron in a blast furnace, which is turned into steel in an oxygen furnace
Scrap EAF: Scrap metal is melted in an electric arc furnace (EAF) using electrical energy
NG DRI-EAF: Iron ore turns into iron using natural gas, which is then melted in an EAF to produce steel
Green H2 DRI-EAF: Green hydrogen replaces natural gas as an iron ore reductant; byproduct is water vs. CO2
Iron ore electrolysis: Molten oxide electrolysis runs a current through iron ore and liquid electrolyte to split ore into pure molten iron; electrowinning-EAF dissolves iron from iron ore in acid, then electrifies it to form solid iron

## Slide 26: Carbon capture, utilization, and storage (CCUS) is an emerging technology that reduces steel’s carbon footprint by capturing released CO2
Iron ore
Iron
Steel
Despite a cited ~90% decarbonization potential, CCUS technology is largely unproven
Sources: World Steel Association; IEEFA (2022); IEA, Iron and Steel Technology Roadmap (2020); Steel Technology, Basic Oxygen Furnace Steelmaking; Recycling Today, Growth of EAF Steelmaking; Wildsight, Do We Really Need Coal to Make Steel. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Less viable for the blast furnace route given difficulty of capturing all carbon released
Capture rates range from 50%-90%, and viability is debated due to the lack of a single capture point
3
Observations
BF-BOF: Iron ore, coke, and limestone produce iron in a blast furnace, which is turned into steel in an oxygen furnace
Scrap EAF: Scrap metal is melted in an electric arc furnace using electrical energy
NG DRI-EAF: Iron ore turns into iron using natural gas, which is then melted in an EAF to produce steel
Green H2 DRI-EAF: Green hydrogen replaces natural gas as an iron ore reductant; byproduct is water vs. CO2
Iron ore electrolysis: Molten oxide electrolysis runs a current through iron ore and liquid electrolytes to split ore into pure molten iron; electrowinning-EAF dissolves iron from iron ore in acid, then electrifies it to form solid iron
CCUS: Equipment is added to existing steel-producing infrastructure to capture emitted CO2, to then sequester or reuse

## Slide 27: Green H2, electrolysis, and CCUS could reduce steelmaking CO2 emissions by over 85% if implemented at scale
 | 100% Green Hydrogen (H2) DRI-EAF | Iron Ore Electrolysis | Carbon Capture, Utilization, and Storage (CCUS)
Description | Green hydrogen replaces natural gas as an iron ore reductant in DRI shaft; the rest of the process remains the same Generates water as a byproduct instead of CO2 | Two different processes are possible: Molten oxide electrolysis: High current runs through mixture of iron ore and liquid electrolyte to split ore into pure molten iron Electrowinning-EAF: Iron from iron ore is dissolved in acid. Iron-rich solution is then electrified to form pure solid iron | CCUS equipment can be added to existing steel-producing infrastructure to capture emitted CO2 Captured CO2 is then sequestered underground or reused
Real-time sector initiatives | HYBRIT 100% fossil fuel-free DRI-EAF production with green H2 used for DRI | Electra Electrowinning to produce high-purity iron plates ready for EAF input (no DRI or MOE step) | ArcelorMittal Carbalyst® captures carbon from a blast furnace and reuses it as bio-ethanol. However, technology not proven at scale
Applicability to conventional routes | Applicable to existing DRI-EAF route, with minor retrofitting | Full overhaul of BF-BOF equipment required; replacement of DRI shaft in DRI-EAF | Retrofitting of capture technology is possible on conventional BF-BOF and DRI-EAF
Decarbonization potential (vs. BF-BOF) | ~90% | ~97% | ~90%
Estimated production cost (excl. CapEx) | <$800 per tonne of steel | ~$215 per tonne of iron + cost of ‘stranded’ iron ore | ~$380 – 400 per tonne
3
2
1
Sources: Columbia Center on Global Energy Policy (2021); IEA, Iron and Steel Technology Roadmap (2020); McKinsey (2020); Mining Technology (2023); Tata Steel; Primetals Technologies;
Edie, ArcelorMittal accused of net-zero greenwashing (2023). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (13 March 2024); share/adapt with attribution.
Contact: gwagner@columbia.edu
Hypothetical best-case scenario

## Slide 28: In green hydrogen DRI-EAF, hydrogen replaces natural gas as reductant to create pure iron, with water as the main byproduct
100% Green H2 DRI-EAF production process
Source: Columbia Center on Global Energy Policy (2021), HYBRIT, HYBRIT Media Bank, World Economic Forum (2021), Department of Energy. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Source: HYBRIT
Description
Hydrogen is used as a reductant instead of natural gas to transform iron ore into solid, purified iron. After this, the iron is moved to an electric arc furnace where it is transformed into crude steel
Instead of CO2, the main byproduct of this production process is water
For the process to be CO2 neutral, two important criteria must be met
  The electricity used to power the electric arc furnace should come from a renewable source
  The hydrogen used in the production process should be green hydrogen
Hydrogen sourcing
Hydrogen can be produced in several ways, not all of which are CO2 neutral
Green hydrogen: produced from water electrolysis using 100% renewable electricity – zero-carbon option
Grey hydrogen: produced from natural gas, methane, or other carbon-containing feedstock
Blue hydrogen: similar to grey hydrogen, but with carbon capture (capture rate of 85-95%) – low-carbon, but not zero-carbon, option

## Slide 29: Global green hydrogen production needs to expand significantly for green hydrogen DRI-EAF to become feasible
Chart: 
 | 57 | 99 | 123 | 103 | 92
 | 115 | 191 | 283 | 400 | 506
0
100
200
300
400
500
600
Low and zero-carbon hydrogen production for Net Zero scenario by Deloitte, 2030-2050 (in mm tonnes)
2030
2035
2040
2045
2050
172
290
406
503
598
Green hydrogen
Blue hydrogen
Green hydrogen production needs to grow at a rapid rate
Source: Deloitte Green hydrogen: Energizing the path to Net Zero (2023), Washington Post (2023), IRENA (2021). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Observations
Hydrogen already produced commercially today, but currently only 1% produced using renewable energy
New green hydrogen production should be built close to renewable energy suppliers like solar and wind farms
  Production can then even be synced to ramp up when solar and/or wind energy is available
Strong policy support for green hydrogen is expected to help scaling efforts. For example, in the US tax code section 45V provides tax credits for hydrogen production
Blue hydrogen production projected to grow in regions with abundant natural gas resources to help kickstart the global hydrogen economy. Peak production expected in 2040

## Slide 30: Molten Ore Electrolysis uses electricity to transform iron ore into pure molten iron ready for refining
Source: Boston Metal, Mining Technology (2023), Mission Possible Partnership Net Zero Steel Sector Transition Strategy (2021)
Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Molten Ore Electrolysis (MOE) is a one-step steelmaking process
Source: Boston Metal
Process description
In a Molten Ore Electrolysis (MOE) reactor, iron ore is combined with an electrolyte, and a strong electrical current is applied to initiate the electrolysis process
The result of this process is molten iron, which is immediately suitable for transfer to the refining stage. In this subsequent stage, carbon and other elements are added to transform the molten iron into refined steel
The only significant byproduct from this process is oxygen (O2), coming from the iron oxide in the iron ore
MOE power consumption per tonne of steel (13 GJ / tonne) is considerably less than that of BF-BOF (24 GJ / tonne)
For the process to be completely carbon neutral, electricity used to power the reactor should come from renewable sources

## Slide 31: In electrowinning-EAF, an iron-rich solution is electrified to create pure grade iron ready to be used in an electric arc furnace
Source: Lopes et al. (2022), Mining Technology (2023), Mission Possible Partnership Net Zero Steel Sector Transition Strategy (2021)
Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Electrowinning produces pure iron at low temperatures ready for EAFs
Source: Electra
Process description
Iron ore is dissolved into an acid to create a stable iron-rich liquid while removing ore impurities. An electric current is then applied to extract iron from this liquid, releasing oxygen but no CO2
Electrowinning at 60°C (140F), enables low-cost intermittent renewables and energy demand responsiveness, lowering OpEx.
High-impurity, otherwise stranded ores (> 1 billion tonnes available globally) lower OpEx and CapEx in the ore-to-metal value chain, producing co-product revenue
Product is 99.9% pure iron metal, allowing for premium steelmaking with contaminated scrap in EAFs at lower costs

## Slide 32: Carbon capture and storage technologies available, but CCUS remains unproven for use on blast furnaces
Captured carbon either stored or used as feedstock
Sources: IEA Energy Technology Perspectives (2020), IEA Transforming Industry through CCUS (2017), IEA Iron and Steel Technology Roadmap (2020), Global CCS Institute (2017), MIT (2021),
International Journal of Greenhouse Gas Control Volume 61 (2017), IEA Greenhouse Gas R&D Program (2017), Primetals Technologies, Edie – ArcelorMittal accused of net-zero greenwashing. Credit:
Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Source: IEA
Carbon capture
In theory, point capture technologies can be retrofitted onto BF-BOF and DRI-EAF
CO2 is primarily captured from the shafts of both Blast Furnaces and Direct Reduced Iron reactors, and at the end of the crude steelmaking process
Capture rates up to 90%, but efficacy varies, with some systems as low as 50%
Carbon utilization and storage
CO2 is commonly stored in rock formations deep underground to ensure long-term sequestration
While the majority of captured CO2 is currently used for enhanced oil recovery, other emerging applications include feedstock for synthetic fuels, chemicals, and building materials
CCUS Drawbacks
Despite CCUS innovation, viability of CCUS for blast furnace is hotly contested due to absence of a single, harnessable carbon egress point on a blast furnace and the scarcity of pure carbon
  Despite a few small pilot projects, no full-scale CCUS facilities for blast-furnace steelmaking are operational anywhere

## Slide 33: Green H2, electrolysis, and CCUS could reduce steelmaking CO2 emissions by over 85% if implemented at scale
Sources: Columbia Center on Global Energy Policy (2021); American Institute of Chemical Engineers (2023); Electra; Boston Metal; Midrex (2021); International Journal of Greenhouse Gas Control Volume 61 (2017); Mission Possible Partnership Net Zero Steel Sector Transition Strategy (2021). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Chart: 
 | 89.84 | 97 | 90
 | 85 | 95.57 | 90
0
20
40
60
80
100
Crude steelmaking CO2 emissions reduction potential of deep decarbonization technologies relative to conventional BF-BOF and NG DRI-EAF routes (in %)
Green H2 DRI-EAF
(Zero-carbon elec.)
Electrolysis
(Zero-carbon elec.)
CCUS Additions
97
96
CO2 Reduction Potential (vs. Conventional BF-BOF)
CO2 Reduction Potential (vs. Conventional NG DRI-EAF)
All discussed technologies have a CO2 reduction potential of >85%
  Hypothetical best-case scenario
Observations
A key enabler for green steel production is an abundance of green electricity, which is required for both powering electrolysis and the production of green hydrogen
  Assuming the current global electricity mix does not change, H2 DRI-EAF would have a decarbonization potential of only 60% instead of >85% when 100% green electricity is used
The 90% CO2 reduction for CCUS is a hypothetical best-case scenario, which at present has not been proven at scale

## Slide 34: Steel decarbonization technologies, however, often come with a green premium and require large amounts of green energy
Chart: 
 | 800 | 400 | 380 | 365 | 325 | 215
200
400
600
800
1,000
0
Green H2 DRI-EAF
Average steel production cost estimates per technology (excluding CapEx) at current price levels (USD per tonne)
CCUS (BF-BOF)
DRI-EAF
BF-BOF
Electrolysis
~380
~365
CCUS (DRI-EAF)
Note: Electrolysis costs are assumed to see a 15% reduction relative to BF-BOF. Carbon capture costs as $25/tonne-CO2 with a ~90% capture rate. Green H2 price at $6.40/kg. Sources: Columbia Center on Global Energy Policy (2021); Boston Metal; MIT (2018); Journal of Cleaner Production Volume 389 (2023); IEA, Is carbon capture too expensive? (2021); McKinsey (2020); Nature Energy (2022); IEA, Iron and Steel Technology Roadmap (2020). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (13 March 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Decarbonization technologies
Conventional technologies
Green technologies often come at a green premium
  Hypothetical best-case scenario
Observations
Green H2 DRI-EAF
Green H2 prices are expected to fall >50%, to $2.20-$2.90 per kg by 2030, making H2 DRI-EAF adoption much more attractive
Switching from BF-BOF to green H2 DRI-EAF is costly without government support. CapEx required for a new plant ranges from $1.1 billion to $1.7 billion and operating expenses are higher
Electrolysis/Electrowinning
Claimed cost savings compared to conventional steel production methods are still uncertain due to the nascency of technology
At present, there is not enough green electricity available on grids to support large-scale electrolysis-based steelmaking
CCUS
According to the IEA, CCUS retrofits are at present the most advanced and cost-effective low-carbon solutions for the steel industry
Adding CCUS technology to existing plants is expected to require only minor modifications

## Slide 35: Other transitional decarbonization technologies take less time and effort to implement but have lower decarbonization potential
 | MODIFICATIONS TO BF-BOF / DRI-EAF PROCESSES |  |  | NEW PRODUCTION PROCESS
 | Biomass as input | Switch to zero-carbon electricity | Partial green hydrogen injections | Smelting Reduction BOF (SR-BOF)
Process description | Biomass used as substitute for coal in BF-BOF Biosyngas used as substitute for natural gas in DRI shaft | Switch from fossil-fueled electricity to 100% green electricity >60% electricity generation is fossil fuel-based today | Injection of hydrogen (~5-10%) to reduce coal use in BF Injection of hydrogen (~30%) to reduce natural gas use in DRI shaft | Production process that eliminates need for coke making and iron ore sintering Emits less CO2 than regular BF-BOF
Decarbonization potential (vs. BF-BOF) | ~40% | ~5 – 40% | ~20% | ~20%
Estimated production costs / tonne (excl. CAPEX) | ~$455 – 700 | ~$345 – 435 | ~$375 – 495 | ~$310
Limits to decarbonization | Insufficient sustainable biomass is likely available to enable a global transition to this production method | Direct process emissions from BF-BOF and DRI-EAF are not addressed | There is a limit to how much H2 can be injected without replacing production equipment | Coal, a primary input, emits CO2, but smelting reduction-BOF provides a concentrated CO2 stream, ideal for capture
Source: IEA Iron and Steel Technology Roadmap (2020), World Steel Association (2021), Energy Institute Statistical Review of World Energy (2023), Columbia Center on Global Energy Policy (2021)
Journal of Cleaner Production Volume 393 (2023). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution.
Contact: gwagner@columbia.edu

## Slide 36: Transitional decarbonization technologies only achieve CO2 reductions of up to 50%
Note: methane leakage not accounted for in gas substitution methods. Source: Columbia Center on Global Energy Policy (2021), MIDREX (2020), Tata Steel Europe (2020). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Chart: 
 | 38.3 | 7.4 | 21.4 | 20
 | 53.7 | 40.6 | 26.16 | -18
0
20
40
60
80
100
-20
CO2 emissions reduction potential relative to conventional BF-BOF and NG DRI-EAF routes (in %)
10% Green H2
BF-BOF
30% Green H2
DRI-EAF
Smelting Reduction - BOF
Biomass Input
Zero-Carbon Electricity Switch
38
-18
CO2 Reduction Potential (vs. Conventional BF-BOF)
CO2 Reduction Potential (vs. Conventional NG DRI-EAF)
Transitional technologies have limited decarbonization potential
Observations
Switching to biomass input assumes the use of sustainably-sourced biomass. Using biomass with large carbon footprint will offset achieved reductions
Switching to zero-carbon electricity sources is necessary to power deep decarbonization technologies such as electrolysis, but switching to zero-carbon electricity alone will only have limited effect
Replacing a BF-BOF setup with a smelting reduction-BOF route requires high CAPEX and still emits more CO2 than DRI-EAF
  However, CO2 stream from smelting reduction-BOF is typically highly concentrated, making it ideal for carbon capture

## Slide 37: Transitional technologies also come with green premiums, possibly locking in uneconomical pathways
Note: assumes hydrogen price of $6.64 per kg. Source: Columbia Center on Global Energy Policy (2021), MIDREX (2020), IEA Iron and Steel Technology Roadmap (2020). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Most transitional technologies also have considerable green premiums
Chart: 
 | 325 | 505 | 345 | 450 | 310
0
1,000
250
500
750
Avg. steel production cost estimates (excl. CAPEX) for transitional technologies applied to BF-BOF (in USD / tonne)
BF-BOF
10% green H2 BF-BOF
Zero-carbon electricity (BF-BOF)
Biomass (BF-BOF)
Smelting Reduction BOF (BF-BOF)
~450
Conventional technologies
Transitional technologies
Chart: 
 | 365 | 495 | 435 | 700 | 310
0
1,000
250
500
750
Avg. steel production cost estimates (excl. CAPEX) for transitional technologies applied to DRI-EAF (in USD / tonne)
DRI-EAF
30% green H2 DRI-EAF
Zero-carbon electricity (DRI-EAF)
Biomass (DRI-EAF)
Smelting Reduction BOF (DRI-EAF)
~700
~365
~435
Observations
DRI-EAF sees a higher jump in costs when switching to zero-carbon electricity than BF-BOF because the Electric Arc Furnace (EAF) runs only on electricity
To use biomass in the DRI-EAF process biomass has to be gasified to turn it into biosyngas, which leads to higher estimated costs
A number of these transitional technologies result in higher production costs per tonne of steel than when CCUS is installed on BF-BOF or DRI-EAF
  It is however important to again note that CCUS for blast furnaces has not yet been proven to work at scale
  Furthermore, these numbers do not include CAPEX, which is likely to be considerable for a CCUS installation

## Slide 38: Adoption trends & obstacles

## Slide 39: Key messages Steel’s future
Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Reaching net zero by 2050 would require a ~25% emissions reduction by 2030
Policymakers can and should step in to assist with green technologies, such as H2 Green Steel’s and Electra’s new generation plants
The focus should be on creating low-cost, low-carbon electricity and on driving down capital costs for new technologies
Time is of the essence, as Asia’s large fleet of high-carbon legacy blast furnaces (~75% of global iron production) are due for costly relining in the next 10 years. This presents an opportunity to instead invest in newer, greener technologies
A production tax credit for low-emission iron would support electrolysis as well as green H2

## Slide 40: BF and EAF, bolstered by China, lead global steel capacity, while other technologies – including clean – constitute <10%
Global steel capacity in 2023: 2.27 billion tonnes
Source: Global Energy Monitor – Global Steel Plant Tracker Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
40%
100%
20%
60%
80%
0%
India 5%
Japan 7%
India 6%
9%
29%
62%
Other
China
15%
Electric Arc Furnace (EAF)
Other
37%
Brazil 1%
Italy 5%
China
53%
Iran 7%
Russia 4%
South Korea 4%
South Korea 4%
Russia 5%
Luxembourg 5%
Japan 7%
Germany 2%
Luxembourg 6%
Other
16%
U.S. 9%
Blast Furnace (BF)
U.S. 13%

## Slide 41: IEA expects technology transition to take off after 2030, and CCUS to play the biggest role in 2050 of all green steel technologies
Chart: 
 | 73 | 59 | 28.62
 | 5 | 8 | 7.02
 | 22 | 3 | 15.66
 | 3 | 2.7
 | 27 | 46
20%
40%
60%
80%
0%
100%
2022
2030
2050
Production of crude steel by technology in IEA net zero scenario, 2022-2050 (in %)
CCUS-Equipped
Electrolysis-Based
NG DRI-EAF
Green Hydrogen DRI-EAF
BF-BOF
Other (inc. Bioenergy)
Scrap EAF
IEA expects scrap steel recycling to play a significant role by 2050
Sources: IEA (2022); IEA, Net Zero by 2050 (2021); IEEFA (2022): Net Zero Steel (2021). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati, and Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Observations
The International Energy Agency (IEA) expects limited decarbonization progress until 2030, with only a slight increase in scrap EAF production and first production using green hydrogen and electrolysis
Scrap steel electric arc furnace (EAF) is expected to become the most used production method for steel by 2050 ─ taking 46% market share
In the IEA’s scenario, the remaining 54% is split between green hydrogen, electrolysis-based production, and CCUS-equipped production
  It should be noted that the effectiveness of carbon capture, utilization, and storage on blast furnaces is still challenged and debated within the steel industry

## Slide 42: Mission Possible Partnership, on the other hand, expects green hydrogen and bioenergy to drive decarbonization
Chart: 
 | 3.13 | 3.13 | 4.25 | 3.47 | 3.03 | 1.1 | 0.25 | 0.25 | 0.25 | 0
 | 1.12 | 0.78 | 0.44 | 1.93 | 0.85
0.25
CO2 removals (e.g. DAC)
Annual iron and steel sector CO2 emissions (Scope 1 & 2) reduction by decarbonization route (in Gt CO2)
2050 Sector Residual Emissions
CCUS
Iron reduction w. natural gas, green hydrogen or bioenergy
Transitional technologies
Increased scrap steelmaking
2050 Emissions (BAU)
BAU emissions increase
2020 Emissions
0.00
Net Zero
Iron and steel sector breakdown of Mission Possible Partnership (MPP) decarbonization route from 2020 to 2050
Notes: BAU = Business as usual, assuming production route mix as of 2020 maintained; Increased scrap steelmaking refers to increase in both Scrap EAF production and use of scrap in primary
production routes; DAC = direct air carbon capture. Sources: Mission Possible Partnership Making Net Zero Steel Possible (2022). Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
The Mission Possible Partnership is an industry coalition aimed at sparking the net-zero transformation of seven industrial sectors (including the steel sector)

## Slide 43: Besides green premiums, there are other barriers preventing the adoption of green steel technologies (1/2)
Sources: IEA CO2 Transport and Storage, IEA Iron and Steel Technology Roadmap (2020), Financial Times (2022), McKinsey (2020), McKinsey Transition to Net Zero: Steel (2022), US DoE Oak Ridge National Laboratory; icons via Noun Project. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Transport and storage cost of CO2
As it relates to global carbon storage, demand is outpacing storage space development
Without increased efforts to accelerate CO2 storage development, the availability of CO2 storage could become a bottleneck to CCUS deployment, alongside aforementioned drawbacks, like unproven technology
Stranded asset risk
Existing conventional plant equipment worldwide has an average age of only 13-14 years (<50% of the typical lifetime of 40 years)
Overhaul of production routes for to transition to Net Zero could result in $345-$518B of stranded assets
Stranded assets expected to be concentrated in Asia, particularly China and India
Infrastructure and equipment risk
Green infrastructure, especially zero-carbon electricity generation and hydrogen production capacity, have to expand significantly to enable the steel industry to transition
Electrolysis technologies are nascent –production equipment still needs to be proven successful at mass scale

## Slide 44: Besides green premiums, there are other barriers preventing the adoption of green steel technologies (2/2)
Sources: IEA CO2 Transport and Storage, IEA Iron and Steel Technology Roadmap (2020), Financial Times (2022), McKinsey (2020), McKinsey Transition to Net Zero: Steel (2022), US DoE Oak Ridge National Laboratory; icons via Noun Project. Credit: Mimi Khawsam-ang, Max de Boer, Grace Frascati & Gernot Wagner (22 February 2024); share/adapt with attribution. Contact: gwagner@columbia.edu
Limited governmental support
Transitioning to new production technologies expected to cost $4.4T over ~30 years
Production costs per tonne of steel could rise by 30% driven by higher OPEX and required CAPEX of green hydrogen and CCUS technologies
At present, there is limited governmental support to incentivize producers to adopt greener production routes
A consensus definition for green steel and iron
Pressing need for unified definition of green steel and green iron, as diverse approaches are currently being pursued
Having shared definitions is crucial, but of course, no single definition can accommodate all perspectives
Dwindling steel workforce
Insufficient educational and training opportunities for the steel industry’s workforce
Declining interest in younger generations to pursue careers in this field
  Those that are interested typically gravitate toward green steel, meaning employees in the grey steel space are dwindling

## Slide 45: Appendix

## Slide 46: Glossary
BAU | Business as usual
BF-BOF | Blast Furnace-Basic Oxygen Furnace
CAPEX | Capital expenditure(s)
CCUS | Carbon capture, utilization & storage
CO | Carbon monoxide
CO2 | Carbon dioxide
CO2e | CO2 equivalent, using global warming potential as conversion factor
DAC | Direct Air Capture
DRI-EAF | Direct Reduced Iron-Electric Arc Furnace production process
EAF | Electric Arc Furnace
EBITDA | Earnings before interest, taxes, depreciation, and amortization
EW-EAF | Electrowinning-Electric Arc Furnace
Gt | Gigatonne, equal to 1 billion metric tonnes
H2 | Hydrogen
IEA | International Energy Agency
HRC | Hot Rolled Coil (type of finished steel product)
MPP | Mission Possible Partnership – industry decarbonization coalition
MOE | Molten oxide electrolysis
NG | Natural gas
NAFTA | North American Free-Trade Agreement
NG | Natural gas
NG DRI-EAF | DRI-EAF production process using natural gas
NZE | Net Zero Emissions
O2 | Oxygen
OECD | The Organization for Economic Cooperation and Development
OPEX | Operational expenditure(s)
SR-BOF | Smelting Reduction-Basic Oxygen Furnace
Tonne | Metric ton